INFORMATION ON DOCTORAL THESIS

1. Full name: Dao Thi Phuong Thao			2. Sex: Female

3. Date of birth: 06 April, 1981				4. Place of birth: Hung Yen

5. Admission decision number: Decision 4761/QĐ-KHTN-CTSV Dated on 29 December, 2011 of the Rector of VNU University of Science

6. Changes in academic process: None

7. Official thesis title: “Synthesis, Characterization, and Structural Studies of Zr(IV) modified the support materials to treat arsenic, selenic in aqueous solution”

8. Major: Environmental Chemistry				9. Code: 62440120

10. Supervisors: Main supervisor: As.Prof.PhD. Do Quang Trung

Supporting supervisor: As.Prof.PhD. Nguyen Van Noi

11. Summary of the new findings of the thesis

• Synthesis of Zr (IV) materials fixed on activated carbon Tra Bac by hydrothermal method using H2O2 and NH3.

• To study of the materials for  adsorption capacity arsenic and initial study of Zr/AC/N material for absorption capacity selenium from solution.

12. Paratical applicability, if any:

Activated carbon Tra Bac are available materials and easy to produce in Vietnam, making simple, consume less power, low cost, high efficiency adsorption therefore potentially subject highly applicable in practice.

13. Further research directions, if any:

- To study of the materials by hydrothermal method using H2O2 and NH3 from different pH conditions.

- The study of materials such as Zr/AC, Zr/AC/H, Zr/AC/N for adsorption capacity organic arsenic.

14. Thesis-related publications:

1. Dao Thi Phuong Thao, Do Quang Trung, Nguyen Van Noi, Nguyen Thi Hong, Nguyen Thi Mai Anh, Nguyen Manh Tuong, Nguyen Tran Hung (2012), “Investigation of  making up an adsorption material for the treatment of arsenic in water by immobilizing Zr(IV) on Muromac B1”, Vietnam Journal of Analytical Sciences 17(1), pp. 46-50.

2. Dao Thi Phuong Thao, Vu Dinh Thao, Do Quang Trung, Nguyen Van Noi, Pham Ngoc Dung (2014), “Adsorption of selenic from aqueous solution by Zr(IV) loaded ion exchange

resin”, Journal of Science and Technology 159, pp.10-14.

3. Dao Thi Phuong Thao, Do Quang Trung, Nguyen Van Noi, Pham Ngoc Dung (2014), “ Investigation of immobilized Zr(IV) on multi wall carbon nanotubes for the treatment of asenic in water”, Vietnam analytical Sciences society 19(1), pp. 38-44.

4. Dao Thi Phuong Thao, Do Quang Trung, Nguyen Van Hoi, Pham Thi Van (2014), “A study on arsenic removal from water by Zr(IV) material immobilized on activated carbon in NH3 medium”, Vietnam Science Technology Review 19, pp. 50-53.

5. Dao Thi Phuong Thao, Do Quang Trung, Nguyen Van Noi, Pham Thi Van (2014), “Investigation of immobilizing Zr(IV) on activated carbon following hydrothermal method with NH3 medium for sorption arsenic in water”, Vietnam Journal of Chemistry 52(5A), pp. 250-254.

6. Dao Thi Phuong Thao, Do Quang Trung, Nguyen Van Noi, Pham Thi Van (2015), “Investigation of the immobilizion Zr(IV) at low concentration on activated carbon following hydrothermal method with NH3 medium for sorption arsenic in water”, Vietnam Science Technology Review  (6), pp. 15-20.

7. Dao Thi Phuong Thao, Do Quang Trung, Nguyen Van Noi, Pham Thi Van (2015), “Investigation of immobilizing Zr(IV) at high concentration on activated carbon following hydrothermal method with H2O2 medium for sorption arsenic in water”, Vietnam Journal of Chemistry 53(1), pp. 124-129.